## Slide 1
Computational Investigation of Li Boracite Li4B7O12Cl and Related Materials as Solid Electrolytes
Yan Li, Cory Lynch, Natalie A. W. Holzwarth
Department of Physics, Wake Forest University, Winston-Salem, NC 27109, USA
240th ECS Meeting 2021
Session A03 - Solid State Batteries 1
DMR-1940324
WFU DEAC cluster

## Slide 2
Li Boracites
BO3 & BO4
Mineral boracites M3B7O13X, where M = Mg, Cr, Mn, Fe, Co, Ni, Zn or Cd, and X = Cl, Br or I
In Li ion conducting compounds, the Li ions are arranged in diffusional channels formed by the B7O12 framework.
Li-containing boracites Li4+xB7O12+x/2X, where 0 1, and X = Cl, Br or I
This talk: Structural and electrolyte properties of Li4B7O12Cl & analogs obtained by ionic substitution

## Slide 3
Summary of computation methods
First principles electronic-structure calculations and materials modeling
https://www.quantum-espresso.org/
https://www.abinit.org/
Density Functional Theory (DFT) and Density Functional Perturbation Theory (DFPT) with the modified Perdew-Burke-Ernzerhof generalized gradient approximation (PBEsol GGA)
The projector augmented wave (PAW) formalism with atomic datasets generated by ATOMPAW code available at http://pwpaw.wfu.edu
Perdew et al., PRL 100, 136406 (2008)
Structural visualization, symmetry identification, X-ray patterns
https://jp-minerals.org/vesta/
http://www.xcrysden.org/
https://stokes.byu.edu/iso/findsym.php
https://www.ccdc.cam.ac.uk/solutions/csd-core/components/mercury/

## Slide 4
Reported structures of Li4B7O12Cl from 1977*
α phase (Exp. R3, No. 146)
Li(24c): 100% occupied
Li(32e): 25% occupied
β phase (P3c, No. 218)
Li(24c): 96.7% occupied
Li(32e): 27.8% occupied
γ phase (F3c, No. 219)
Li(24c): 93.7% occupied
Li(32e): 31.6% occupied
Room T
310 – 348 K
Above 348 K
* The real space groups of the α and β phases are subgroups of F3c.
** The atomic positions for both α and β phases are not known in experiment
Ideal cubic model
8 formula units/cell
Ideal F3c model
Ideal F3c model
Three disordered phases
*Jeitschko et al., Acta Cryst. B33, 2767-2775 (1977)

## Slide 5
Find the ground state structure for α-Li4B7O12Cl
The calculation finds four identical lowest-energy configurations with the rhombohedral R3c (No. 161) symmetry
Cubic F3c model of the α phase
Li(24c): 100% occupied
Li(32e): 25% occupied
Perform geometry optimizations for 28 unique configurations in the primitive cell setting
Li(24c)
B
Cl
Li(32e)
O

## Slide 6
α-Li4B7O12Cl in rhombohedral R3c structure
ap = bp= cp and α = β = γ = θp ≈ 60°
ac = bc= cc and α = β = γ = θc ≈ 90°
Conventional cell
8 formula units
Face-centered primitive cell
2 formula units
Host Li sites
Native Li vacancies
Cl
B-O Wireframe

## Slide 7
α-Li4B7O12Cl in rhombohedral R3c structure
Host Li sites
Native Li vacancies
Cl
Lattice parameters and Li ion fractional coordinates for the R3c structure of α-Li4B7O12Cl, comparing calculated results with the experimental measurements.
*Experimental data taken from Jeitschko et al., Acta Cryst. B. 33, 2767-2775 (1977)
Cal. R3c |  |  |  | Exp. F3c model |  |  | 
Atom | Wyck | f(x, y, z) (conv.) | Occ. | Atom | Wyck | f(x, y, z) | Occ.
Li(1) | 4x6 b | (0.030, 0.245, 0.245) | 1.00 | Li(1) | 24 c | (0.000, 0.250, 0.250) | 1.00
Li(2) | 4x2 a | (0.865, 0.865, 0.865) | 1.00 | Li(2) | 32 e | (0.871, 0.871, 0.871) | 0.25
Vac. Li | 4x6 b | (0.633, 0.635, 0.873) | 0.00 |  |  |  | 
Cal. R3c |  |  |  |  |  |  | 
Atom | Wyck | f(x, y, z) (conv.) | Occ. | Atom | Wyck | f(x, y, z) | Occ.
Li(1) | 4x6 b | (0.030, 0.245, 0.245) | 1.00 | Li(1) | 24 c | (0.000, 0.250, 0.250) | 1.00
Li(2) | 4x2 a | (0.865, 0.865, 0.865) | 1.00 | Li(2) | 32 e | (0.871, 0.871, 0.871) | 0.25
Vac. Li | 4x6 b | (0.633, 0.635, 0.873) | 0.00 |  |  |  | 
Li4B7O12Cl | a = b = c (Å) | α= β = γ (deg)
Cal. R3c | 12.137 | 90.108
Exp.* R3 | 12.141 | 90.084
Exp.* F3c model | 12.141 | 90.000
Li4B7O12Cl | a = b = c (Å) | α= β = γ (deg)
Cal. R3c | 12.137 | 90.108
Exp.* R3 | 12.141 | 90.084
 | 12.141 | 90.000
Primitive cell model
Conventional cell model
B-O Wireframe

## Slide 8
Phase stability of α-Li4B7O12Cl
Where is the total static energy per formula unit of a specific compound. with = Li2O, B2O3, and LiCl represents the compositional ratio of each reference phase for which the total static energy per formula unit is denoted by .
Reaction energy:
Phonon dispersion curves and projected density states of Li4B7O12Cl with frequencies ranging from 0 ~ 1440 cm-1.
Brillouin zone diagram: Hinuma et al., Comp. Mat. Sci. 128, 140-184 (2017). Note that the rhombohedral lattice is described by an equivalent hexagonal system.
Li2O-B2O3-LiCl phase diagram at 0 K and 0 atm

## Slide 9
Nudged Elastic Band (NEB) analysis for α-Li4B7O12Cl
hb: host b-type site; ha: host a-type site
mb: metastable b-type site (native vacancy)
 The concerted migration mechanism reduces the energy barrier for Li ion conduction in α-Li4B7O12Cl.
Direct: ha  mb
Concerted: ha hb & hb mb
NEB: 1Jónsson et al., in Classical and Quantum Dynamics in Condensed Phase Simulations, World Scientific, Singapore (1998)
2Henkelman et al., J. Chem. Phys. 113, 9901-9904 (2000)
Ehb < Eha < Emb
0.33 eV

## Slide 10
Results of molecular dynamic simulations
Model of Li4B7O12Cl crystal cell with superposed Li positions of molecular dynamics simulation at <T> = 1162 K.
Li(6b)
Vacant Li(6b)
Li(2a)
Time-dependent positions of Li ions
mb
ha
hb
Site occupancy factor:
Time-averaged:
T+
T+
*Recall: the three reported forms α (T< 310 K), β (310 K <T < 348 K), γ (T > 348 K) mainly differ in lattice site occupancy.

## Slide 11
Results of molecular dynamic simulations
Materials | Analysis | Samples | Ea (eV) | σ (T = 300 K, S/cm)
Li4B7O12Cl | Cal. | Ideal | 0.34 | 3.83 x 10-4
 | Exp: Ref (A) | Polycrystalline | 0.53 | 1.00 x 10-7
 | Exp: Ref (B) | Single crystal | 0.49 | 0.98 x 10-7
 | Exp: Ref (C) | Polycrystalline | 0.14 | 3.68 x 10-4
 | Cal. | Ideal | 0.84 | 6.58 x 10-12
 | Exp: Ref (A) | Polycrystalline | 1.03 | 2.14 x 10-14
Li5B7O12.5Cl*
*Li5B7O12.5Cl has a similar B-O framework with Li4B7O12Cl but a different ordering of Li ions.
Ref. A: Cales et al., Solid State Commun. 24, 323 (1977)
Ref. B: Jeitschko et al., Acta Cryst. B. 33, 2767-2775 (1977)
Ref. C: Tan et al., ACS Appl. Energy Mater. 2, 5140 (2019).
with
,

## Slide 12
Ionic substitutions in α-Li4B7O12Cl
Li4Al3B4O12Cl
Li4B7S12Cl
B(1)  Al
Li4Al3B4S12Cl
B(1)  Al & O  S
O  S
Predicted in this work
Realized in experiment*
Predicted in this work
Rhombohedral R3c
ap = bp = cp = 9.133 Å
αp = βp = γp = 61.194°
ac = bc = cc = 13.033 Å
αc = βc = γc = 91.022°
Rhombohedral R3c
ap = bp = cp = 10.584 Å
αp = βp = γp = 59.704°
ac = bc = cc = 14.934 Å
αc = βc = γc = 89.743°
Rhombohedral R3c
ap = bp = cp = 11.386 Å
αp = βp = γp = 68.601°
ac = bc = cc = 15.933 Å
αc = βc = γc = 88.771°
Li4B7O12Cl
Rhombohedral R3c
ap = bp = cp = 8.574 Å
αp = βp = γp = 60.124°
ac = bc = cc = 12.137 Å
αc = βc = γc = 90.108°
Original material
*Kajihara et al., Bull. Chem. Soc. Jpn. 90, 1279–1286 (2017)

## Slide 13
Comparison of diffusional properties
NEB energy diagram of concerted migrations
Mean squared displacement (MSD) vs. time interval
583 K
948 K
0.60 eV
0.39 eV
0.30 eV
0.41 eV

## Slide 14
Are the analog compounds stable?
Li4Al3B4O12Cl
Li4B7S12Cl (proposed)
Li4Al3B4S12Cl (proposed)
Kajihara et al., Bull. Chem. Soc. Jpn. 90, 1279–1286 (2017)

## Slide 15
Phonon calculations
0 cm-1 ω(q) 1440 cm-1
0 cm-1 ω(q) 931 cm-1
Li4B7S12Cl
Li4B7O12Cl
Predicated
Known
∆Fvib (T = 300 K) = 1.38 eV/FU

## Slide 16
Summary
The ground state structure of the room-temperature form of Li4B7O12Cl is identified to have rhombohedral R3c symmetry. The phase is estimated to be stable from the analysis of the convex hull approach and of the phonon spectrum.
The NEB calculations indicate that Li ion migration in Li4B7O12Cl most likely proceeds via concerted migration mechanisms involving two host sites and one natural vacancy.
The room-temperature ionic conductivity of Li4B7O12Cl, calculated from the MD simulation results, is on the order of 10-4 S/cm, which is in good agreement with the recent experiment measurement for pure polycrystalline samples.
Consistent with the recent experimental results, our preliminary calculations also find reduced Li ion migration barriers in the partially B-replaced compound Li4Al3B4O12Cl. The studies on predicted compounds Li4B7S12Cl and Li4Al3B4S12Cl also suggest improved Li ion conducting performance compared with Li4B7O12Cl.
The chemical stabilities of the Li4B7S12Cl and Li4Al3B4S12Cl need further investigation.