## Slide 1
DFT simulations of Li-ion conductor Li2(OH)Cl
Jason Howard, Natalie Holzwarth
Acknowledgements
Zach Hood
WFU Deac HPC Cluster
NSF grant DMR-1507942

## Slide 2
Outline
Motivation
Background of material
Low temperature phase structure search
Molecular dynamics simulations of
high temperature phase

## Slide 3
Motivation
Solid state , fast lithium ion conductor
Finding structure for low temperature phase is stepping stone for understanding the phase transition.
related materials
Understanding the structure of the low temperature phase can help to understand the differences in the
phase transitions or lack there of for the related materials
Understanding the properties of diffusion on a disordered lattice is of general interest
In principle the combination of calculated tracer diffusion coefficients and experimentally measured conductivity can allow for a calculation of the Haven ratio.

## Slide 4
Background of Li2OHCl
Two phases orthorhombic -> cubic(disordered) at 312K
Low temperature phase poor Li-ion conductor
Disordered cubic phase is a good Li-ion conductor
Has been cycled with a lithium anode with the apparent creation of stabilizing SEI layer
Hood, Zach et al. , Li2OHCl “Crystalline Electrolyte for Stable Metallic Lithium Anodes”. J. Am. Chem. Soc. 2016, 138, 1768−1771
312K

## Slide 5
Methods
Quantum Espresso QUANTUM ESPRESSO . (Giannozzi et al. JPCM 21, 394402 (2009)
PAW formalism with LDA, data sets generated with ATOMPAW
(Holzwarth et al. CPC 135, 329 (2001)) http://pwpaw.wfu.edu

## Slide 6
Low Temperature structure
Cubic high temp phase
Orthorhombic, diffraction peaks available but no cif file as of yet
Rapid change in conductivity orthorhombic -> cubic indicates order-> disorder transition of lithium sites
Schwering et. al. has experimentally predicted lattice parameters
Schwering, Georg CHEMPHYSCHEM 2003, 4, 343 - 348
My DFT studies predict a tetragonal ground state , a Orthorhombic structure slightly higher in energy is also predicted
a
b
c
Li-vacancy
Li
O
Cl
H
0.02 eV + Eo
Eo
Tetragonal
Orthorhombic
Yutao Li et al
International Edition: DOI: 10.1002/anie.201604554

## Slide 7
Lattice parameters and XRD
Orthorhombic phase lattice parameters reported by Schwering et al. In angstrom
  a – 3.82 b – 7.998 c – 7.74, ( b/2 = 3.999, c/2 = 3.87) Schwering, Georg CHEMPHYSCHEM 2003, 4, 343 - 348
Tetragonal lattice parameters (DFT) Orthorhombic lattice parameters (DFT)
  a – 3.89 b – 3.89 c – 3.66 a – 3.83 b – 7.97 c – 3.6 (if scaled by 1.08 c = 3.81)
LiCl
DFT tetragonal a, b, c scaled by 1.02
DFT orthorhombic a, b, c scaled 1.02
Hood, Zach et al. ,. J. Am. Chem. Soc. 2016, 138, 1768−1771

## Slide 8
LiCl
Azuma et al report and underestimation of up to 8% in the axis along the OH bond in
Azuma et al , Computational and Theoretical Chemistry 963 (2011) 215–220
Candidate DFT orthorhombic with a-axis and b-axis scaled by 1.02 and c-axis scaled by 1.08
DFT Orthorhombic a, b scaled 1.02, c scaled 1.08
Hood, Zach et al. ,. J. Am. Chem. Soc. 2016, 138, 1768−1771

## Slide 9
Molecular Dynamics of disordered cubic phase
Started from randomly placing lithium on available sites
Used the micro-canonical ensemble , 1 shifted Kpoint, Ecut 45ryd, 1fm second t-step
“Scatter” plots of Lithium and hydrogen positions
Li
O
Cl
H
Li vacancy
a
b
c
b

## Slide 10
Goals of MD simulations
Avg Temp 630K
24ps
3.25
Calculate tracer diffusion coefficients from slopes of mean square displacement vs time plots
  MSD(t) = vs t
24ps
3.25
Tracer diffusion coefficients are related to the ionic conductivity by the equation
where - tracer diffusion coefficient
G.E. Murch Solid State lonics 7 (1982) 177-198
- density of mobile ions per unit volume , - fundamental charge, – Boltzmann constant
– temperature , - the Haven ratio
MSD(t)

## Slide 11
MSD continued
340K
380K
430K
490K
540K
580K
635K
1.6
0
25ps
1.6
0
25ps
340K
380K
430K
490K
540K
580K
635K
*T) vs
2.5 log(
0.5 log(
0.004
0.001
Initial #1
Initial #2
(Initial #1)

## Slide 12
Conclusions
T = 0K ground state predicated to be tetragonal
A candidate structure is found for the low temperature Orthorhombic structure
MD simulations show Lithium hopping that corresponds to the proposed model
for lithium jumps
Hydrogen positions qualitatively correlated with Li vacancies
Measurable diffusion occurring ~350K-650K but results are not converged enough to produce accurate Arrhenius plots

## Slide 13
Internal energy, kinetic energy, total energy and temperature
In Micro Canonical Ensemble
MSD(t) =
1.2
19ps
Kinetic ( ) and internal ( )
0.75
0.65
0.55
19ps
Temperature
19ps
600K
500K
350K
kinetic + internal
19ps
0.015
0.01
0.0

## Slide 14
time avg kinetic and internal
0.68
0.61
0.64
19ps
time avg temperature
19ps
535K
520K
500K

## Slide 15
Order parameter analysis
Avg Temp 630K
24ps
3.25
MSD(t) =
0.44
24ps
0.36
Need a parameter that can gauge if the simulation is long enough
Define where if a lithium is occupying the site at time
    0 if a lithium is not occupying the site at time
Because each site should be equally occupied and there are 3 sites for every 2 lithium's
at long
For a supercell this leads to for long . The index is for the possible Li sites in simulation cell

## Slide 16
Effective temperature in the Micro canonical ensemble
Tempurature flucates in MD simulation in small(not in Thermodynamic limit) supercell
Calculated diffusion constants are an average over a range of temperatures
Where probability of the Temperature T during the run.
is an effective temperature for the run